DURAL 100

Precast Segmental Epoxy Adhesive

DURAL 100 is a two component, 100% solids, moisture insensitive adhesive for use as a bonding agent for precast segmental box girders, bridge and other segmental construction.

{Note to Specifier: The paragraphs below are meant to be incorporated into Parts 2 and 3 of a standard CSI 3 Part Format specification, project’s General Structural Notes or directly onto the plans. They must be carefully reviewed by a qualified design professional and edited to meet the particular requirements of the project at hand, assure compliance with any governing building codes, and coordinate with other specification sections and drawings.}

PART 2:	PRODUCT

2._     EPOXY ADHESIVE

A.	Two component, pre-proportioned, moisture insensitive, VOC compliant, 100% solids epoxy adhesive. Products shall conform to:

ASTM C 881 Type VI, Grade 3, Classes D, E, F.

Material shall have the following properties:

1. 	Class D Minimum 6,000 psi Compressive Yield

2. 	Class E Minimum 6,800 psi Compressive Yield

3.	Class F Minimum 6,300 psi Compressive Yield

4. 	Product:

- Euclid Chemical Company (The); Dural 100 Precast Segmental Epoxy Adhesive.

- www.euclidchemical.com

{Note to Specifier: Based on the actual application temperature, select the appropriate Class [D, E, F] to suit job conditions.}

B.	Manufacturer shall have ISO 9001 Quality Certification. To ensure compatibility all 	products shall be from the same manufacturer.

PART 3:	EXECUTION

3._ 	EXAMINATION

A. 	Examine concrete surfaces to receive epoxy bonding agent. Notify Engineer if surfaces are not acceptable. Do not begin surface preparation or application until unacceptable conditions are corrected.

3._	SURFACE PREPARATION

A.	The surface must be dry and structurally sound. The substrate must also be free of all dust, dirt, grease, oil, coatings, laitance and other contaminants that would interfere with proper adhesion. The surface should be lightly sand blasted, shot blasted or water blasted with a minimum pressure of 5,000 psi (34.5 MPa). Wet surfaces must be dried. Remove all visible water with a heater and/or oil-free air compressor. Any dust that may have accumulated between cleaning and application of DURAL 100 should be removed by an oil-free air compressor.

3._	APPLICATION

A.	Mix and place epoxy adhesive in accordance with manufacturer’s written instructions.