GUIDE SPECIFICATION

EUCOWELD 2.0

Latex Bonding Agent for Concrete Repairs and Toppings

EUCOWELD 2.0 is a liquid latex bonding agent for cement-based repair mortars and concrete. EUCOWELD 2.0 has a long open time, and repair materials can be placed either after it has dried, or while it is still wet. This bonding agent represents a new generation of easy-to-use latex, which exhibits drastically improved performance and stability in comparison to the typical re-wettable ethylene vinyl acetate (EVA) bonding agents currently available. EUCOWELD 2.0 is a unique, non-EVA based latex that utilizes reactive chemistry for bonding, rather than depending on the moisture content of the repair material.

{Note to Specifier: The paragraphs below are meant to be incorporated into Parts 2 and 3 of a standard CSI 3 Part Format specification, project’s General Structural Notes or directly onto the plans. They must be carefully reviewed by a qualified design professional and edited to meet the particular requirements of the project at hand, assure compliance with any governing building codes, and coordinate with other specification sections and drawings. In no case shall these Guide Specifications be considered to be Contract Documents or serve as installation instructions for the product being discussed. In any cases of discrepancy the manufacturer's most recently published data sheet shall take precedent.}

PART 1.0	GENERAL

1.01 	RELATED WORK:

A. 	Joint Fillers – Eucolastic, Dural 340, Qwikjoint UVR

B. 	Concrete Repair:

1. 	Vertical and Overhead: EucoRepair V100, Tamms Structural Mortar

2. 	Horizontal: Express Repair, VersaSpeed LS100 or VersaSpeed 100

3. 	Form and Pour: Eucocrete

C. 	Crack Repair/Injection: Dural 452 LV, Dural Fast Set Epoxy Gel

D. 	Bonding Agents: Eucoweld 2.0, Duralprep A.C., Dural 452 MV, EucoFloor Epoxy Primer

E. 	Waterproofing/Dampproofing : Tamoseal, Vandex Super, Hey’Di K-11, Vandex BB75

F. 	Architectural Coatings: Tammscoat, Tammolastic

G. 	Anti-Graffiti Coatings:  AG 100,

H. 	Traffic Deck Coatings: Tammsdeck, Flexdeck

I. 	Decorative Floor Coatings: Duraltex

J. 	Epoxy Chemical Resistant Coatings: Duralkote 240, Duralkote 500, Duraltex 1705/07, Duraltex 1805/07

K. 	Penetrating Water Repellents:

1. 	Horizontal and Vertical: Baracade Silane 40 WB, Baracade WB 244, Baracade Silane 100 C, Baracade Silane 40 IPA,

2. 	Vertical: Chemstop WB Regular/Heavy Duty

L. 	Penetrating Epoxy Sealer: Euco #512 VOX Epoxy Sealer

M. 	Cathodic Protection: Sentinel Galvanic Anodes

PART 2.0	PRODUCTS

2.__	BONDING AGENT/PRIMER

A.	Surface-Applied Styrene Acrylate Bonding Agent, Non-Redispersible: ASTM C1059/C1059M, Type II manufactured to allow placement of cementitious materials while bonding agent is still wet or up to 7 days later at 70 deg F. Provide product suitable for use interior and exterior and suitable for repairs that will be frequently wet or submerged after curing.

1.	Basis of Design Product: Euclid Chemical Company (The): EucoWeld 2.0

2.	VOC Content: Less than 5 g/L.

3.	ASTM C1583 Direct Tension Bond Strength: Minimum 370 psi (2.55 MPa) at 7 days.

4.	ASTM C882 Slant Shear Bond Strength: Minimum 2760 psi (19 MPa) at 14 days wet.

PART 3.0	EXECUTION

3.___	BONDING AGENT APPLICATION

A.		Apply all prepackaged bonding agent materials within recommended ambient and substrate temperatures published in writing by manufacturer.

B.		Do not apply materials over frozen or frost filled surfaces.

C.		Upon completion of all concrete removal, reinforcing steel preparation, concrete surface preparation, and cleaning operations apply specified bonding agent to substrate. Provide complete and thorough coverage of surface ensuring that bonding agent has been fully worked into profile of surface.

D.		Apply specified surface applied styrene acrylate bonding agent in accordance with manufacturer’s written recommendations where indicated.

E.		Special attention is to be paid to timing of placement of mortar scrub coats and bonding agents with regards to allowable open time of all bonding materials. Assure that placement of subsequent repair mortar is able to be made within open-time of any bonding agents, or while any mortar scrub coats are still wet and have not yet stiffened.

END GUIDE SPEC