PSI FIBERSTRAND 150

Polypropylene Synthetic Micro-Fiber

{Note to Specifier: The paragraphs below are meant to be incorporated into Parts 2 and 3 of a standard CSI 3 Part Format specification (normally 03 30 00), the General Structural Notes, or directly onto the plans. They must be carefully reviewed and edited by a qualified design professional to meet the requirements of the project and governing building codes. Coordinate with other specification sections and drawings.}

PART 2:	PRODUCTS

2.__	SYNTHETIC MICRO-FIBER

A.	100% virgin multifilament polypropylene fibers complying with ASTM C 1116/C 1116M 4.1.3. Available in ¼ inch (6 mm),  ¾ inch (19 mm), and multi-length blend (ML). Minimum  fiber count for the ML of 54 million fibers per pound.

1.	Product:

a)   Euclid Chemical Company (The); PSI Fiberstrand 150;

www.euclidchemical.com.

- Fiber manufacturer shall have ISO 9001 certification.

2._	CONCRETE  MIXES

- A.	Use Synthetic Micro Fibers at rate of [0.67][1.0] (1.5) [Select dosage rate] pounds per cubic yard of concrete.

PART 3:	EXECUTION

3._	SYNTHETIC MICRO FIBERS

- Synthetic Micro Fibers:  Add to concrete and mix for 3 – 5 minutes to provide uniform distribution.

- For broomed surfaces, broom once in one direction only.