PSI FIBERSTRAND F

Fibrillated Polypropylene Micro-Fiber

{Note to Specifier: The paragraphs below are meant to be incorporated into Parts 2 and 3 of a standard CSI 3 Part Format specification (normally 03 30 00), the General Structural Notes, or directly onto the plans. They must be carefully reviewed and edited by a qualified design professional to meet the requirements of the project and governing building codes. Coordinate with other specification sections and drawings.}

PART 2:	PRODUCTS

2.__	FIBRILLATED  MICRO-FIBER

A.	100% virgin fibrillated polypropylene fibers complying with ASTM C 1116, C 1116M 4.1.3. Available in ¼ inch (6 mm), ½ inch (13 mm), ¾ inch (19 mm), 1.5 inch (38 mm), 2 inch (51), and multi-length blend (ML).

1.	Product:

a)   Euclid Chemical Company (The); PSI Fiberstrand F;

www.euclidchemical.com.

- Fiber manufacturer shall have ISO 9001 certification.

2._	CONCRETE  MIXES

- A.	Standard application rate for Fiberstrand F is 1.5 pounds per cubic yard of concrete however lower dosage rates may be acceptable depending on local building codes. Higher dosage rates can also be used, contact your Euclid representative regarding the specific application.

PART 3:	EXECUTION

3._	FIBRILLATED MICRO-FIBER

- Fibrillated Micro-Fiber:  Add to concrete and mix for 3 – 5 minutes to provide uniform distribution.

- For broomed surfaces, broom once in one direction only.