PSI FIBERSTRAND MULTI-MIX 80

Fine Denier Polypropylene Micro-Fiber

{Note to Specifier: The paragraphs below are meant to be incorporated into Parts 2 and 3 of a standard CSI 3 Part Format specification (normally 03 30 00), the General Structural Notes, or directly onto the plans. They must be carefully reviewed and edited by a qualified design professional to meet the requirements of the project and governing building codes. Coordinate with other specification sections and drawings.}

PART 2:	PRODUCTS

2.__	FINE DENIER POLYPROPYLENE MICRO-FIBER

A.	Fine denier 100% virgin multifilament polypropylene fibers complying with ASTM C 1116,C 1116 M 4.1.3. Available in ¼ inch (6 mm), ½ inch (13 mm).

1.	Product:

a)   Euclid Chemical Company (The); PSI Fiberstrand Multi-Mix 80;

www.euclidchemical.com.

- Fiber manufacturer shall have ISO 9001 certification.

2._	CONCRETE  MIXES

- A.	Use Fine Denier Polypropylene Micro-Fibers at rate of 0.5 pounds per cubic yard of concrete.

PART 3:	EXECUTION

3._	FINE DENIER POLYPROPYLENE MICRO-FIBER

- Fine Denier Polypropylene Micro-Fiber:  Add to concrete and mix for 3 – 5 minutes to provide uniform distribution.

- For broomed surfaces, broom once in one direction only.