EUCO TREMIE GROUT

Non-Metallic, Non-Shrink Underwater Grout

{Note to Specifier: This add-in specification component specifies Euclid Chemical Company, EUCO TREMIE GROUT- Non-Metallic, Non-Shrink Grout.  EUCO TREMIE GROUT is designed for underwater grouting applications. EUCO TREMIE GROUT is highly flowable and remains cohesive when placed and pumped in offshore grouting applications. It contains only natural aggregate and an expansive cementitious binder.}

{Note to Specifier: The paragraphs below are meant to be incorporated into Parts 2 and 3 of a standard CSI 3 Part Format specification, project’s General Structural Notes or directly onto the plans. They must be carefully reviewed by a qualified design professional and edited to meet the particular requirements of the project at hand, assure compliance with any governing building codes, and coordinate with other specification sections and drawings.}

1.1	QUALITY REQUIREMENTS

A.	Manufacturer: ISO 9001 quality certified as primary manufacturer of specified products.

1.2	INFORMATIONAL SUBMITTALS

A.	Product List: List manufacturer name and product name for each product proposed for use as cementitious grout.

B.	Manufacturer Certificate: Indicating products listed on Contractor's Product List are compatible and suitable for the specified application.

PART 2:	PRODUCTS

2.1	MANUFACTURERS

A.	Manufacturer: Provide listed products of Euclid Chemical Co., Cleveland, OH; www.euclidchemical.com.

B.	Manufacturer Single Source: Provide cementitious grout products from a single qualified manufacturer.

2.2	CEMENTITIOUS GROUT

A.	Cementitious Grout:  Cementitious grout for high performance applications.

1.	Product shall conform to:

a)	CRD C621, US Army Corps of Engineers Specification for Non-Shrink Grout

b)	ASTM C1107, Standard Specification for Packaged, Dry, Hydraulic-Cement Grout (non-shrink)

2.	Basis of Design Product:

a)	“EUCO TREMIE GROUT” by The Euclid Chemical Company

b)	Compressive Strength, ASTM C109 Modified to ASTM C1107 Section 11.5, 2 in. (5 cm) cubes:

1)	At 72o F (22o C)

a)	1 day: 3200 psi (22MPa)

b)	3 days: 4800 psi (33 MPa)

c)	7 days: 5600 psi (38 MPa)

d)	28 days: 7200 psi (49 MPa)

2)	At 50o F (10o C)

a)	1 day: 1000 psi (7 MPa)

b)	3 days: 3000 psi (20 MPa)

c)	7 days: 3700 psi (25 MPa)

d)	28 days: 4500 psi (31 MPa)

c)	Volume Change, ASTM C1090 and CRD C621:

1)	At 72o F (22o C)

a)	3 days: 0.04%

b)	7 days:  0.06%

c)	14 days: 0.06%

d)	28 days:  0.08%

d)	Setting time, ASTM C191:

1)	At 72o F (22o C)

a)	Initial set: 5 hours

b)	Final set: 7 hours

2)	At 50o F (10o C)

a)	Initial set: 12 hours

b)	Final set: 18 hours

PART 3:	EXECUTION

{Note to Specifier: This section covers surface preparation, form preparation, mixing, placement, curing, and cleanup for Euclid Chemical’s NS Grout. For complete current instructions and safety information, consult the Technical Data and Material Safety sheets posted at www.euclidchemical.com.  Note: The contractor and engineer are encouraged to consult and review the Euclid Chemical bulletin: “Cementitious Grout Application Guide”:

(http://euclidchemical.com/fileshare/ProductFiles/MiscProductFiles/grout_instructions.pdf.

The document offers instructions detailing the general installation of Euclid Chemical manufactured cement-based grout products. Important: If the contractor is not familiar with standard grout placement techniques, a pre-job meeting is suggested to review the project details unique to the particular job. Contact your local Euclid Chemical representative for additional information}

3.1	SURFACE PREPARATION

A.	All surfaces to be in contact with grout shall be clean and free from rust, grease or oil.

3.2	MIXING

A.	All grouting materials shall be 50°F to 80°F (10°C to 27°C) immediately prior to mixing.

B.	Mix grout in accordance with manufacturer’s written instructions. Mix small quantities with a drill and "jiffy" mixer. Use a paddle type mortar mixer for large jobs.

C.	Charge mixing vessel with appropriate amount of clean, potable water for batch size and then add dry grout. Do not exceed water content recommended by manufacturer. Control water content. Do not add admixtures, sand or cement to grout.

D.	Mix for a minimum of 3 minutes.

3.3	PLACEMENT

A.	Place grout in accordance with manufacturer’s written instructions.

B.	Placed mixed grout immediately and continuously.

3.4	CURING

A.	Cure grout in accordance with manufacturer’s written instructions.

3.5	CLEAN UP

A.	Tools and mixer may be cleaned with water.