EucoFloor SL160

Cementitious, pumpable, single component, self-leveling underlayment for easy application at depths ranging from feather edge to 1” neat, over concrete and wooden floors as an underlayment for subsequent placement of floor coverings.

{Note to Specifier: The paragraphs below are meant to be incorporated into Parts 2 and 3 of a standard CSI 3 Part Format specification, project’s General Structural Notes or directly onto the plans. They must be carefully reviewed by a qualified design professional and edited to meet the particular requirements of the project at hand, assure compliance with any governing building codes, and coordinate with other specification sections and drawings.}

PART 2.0:	PRODUCT

2.__	BONDING AGENT/PRIMER

{REPAIR NOTE : Required Bonding Agents}

{Note to Specifier: Certain bonding agents, adhesives and/or primers are recommended with this product. Choose a recommended bonding agent/primer from the data sheet and insert here.

{PRODUCT}

2.__	CEMENTITIOUS REPAIR MORTAR

- Single component, cement based, self-leveling underlayment suitable for applications from featheredge to 1” in depth and requiring only the addition of water. Material shall have the following properties:

1.	Surface Burning Characteristics per ASTM E 84-13a

Flame Spread Index		0

Smoke Developed Index	5

2.	Compressive Strength per ASTM C 109

Age				Strength

4 hours			900 psi

24 hours			2,000 psi

7 days			3,000 psi

28 days			3,500 psi

3. 	Flexural Strength per ASTM C 348

Age				Strength

7 days			550 psi

28 days			600 psi

4. 	Unit weight:			122 lbs. per cu. ft.

5.	Product:

a) Euclid Chemical Company (The); EucoFloor SL160 www.euclidchemical.com

B.	Manufacturer shall have ISO 9001 Quality Certification. To ensure compatibility, all admixtures shall be from the same manufacturer.

C.	To ensure compatibility, bonding agent and curing compound, if used, shall be from same manufacturer as repair mortar.

PART 3.0:	EXECUTION

3.___	SURFACE PREPARATION

{CONCRETE PREP AND CLEANING NOTE}

A.     Concrete Preparation and Cleaning: Areas to receive concrete repair shall be structurally sound and free from deteriorated concrete, dust, dirt, debris, loosened concrete, paint, oil, efflorescence, laitance, and other contaminants, and shall have a minimum Concrete Surface Profile CSP equal to that recommended by the repair mortar manufacturer per ICRI Guideline 310.2.

3.___	REPAIR MORTAR APPLICATION:

{SELF-LEVELING UNDERLAYMENT APPLICATION NOTE}

A.	Self-Leveling Cementitious Material Application: Mix and apply material in continuous manner per manufacturer’s published recommendations so as to provide smooth uniform surface.