EUCOREPAIR V100

Low Shrinkage, Fiber Reinforced, NSF/ANSI Standard 61 Certified Vertical & Overhead Repair Mortar

EUCOREPAIR V100 is a single-component, quick-setting, low shrinkage repair mortar formulated with unique polymers and fiber reinforcement for vertical and overhead repairs requiring high performance.

{Note to Specifier: The paragraphs below are meant to be incorporated into Parts 2 and 3 of a standard CSI 3 Part Format specification, project’s General Structural Notes or directly onto the plans. They must be carefully reviewed by a qualified design professional and edited to meet the particular requirements of the project at hand, assure compliance with any governing building codes, and coordinate with other specification sections and drawings. In no case shall these Guide Specifications be considered to be Contract Documents or serve as installation instructions for the product being discussed. In any cases of discrepancy the manufacturer's most recently published data sheet shall take precedent.}

PART 2.0	PRODUCTS

2.__	BONDING AGENT/PRIMER

{Note to Specifier: Euclid Chemical bonding agents, adhesives and primers can be used to enhance the bond of this repair mortar. If desired choose a recommended bonding agent/primer from the data sheet and insert product description here. (Note: Latex additives will increase the volumetric resistivity of the mortar making it no longer compatible with Galvanic Anode Protection}

2.__	CEMENTITIOUS REPAIR MORTAR

A.	Trowelable Vertical and Overhead Repair Mortar: Cement-based, one component, low shrinkage, polymer modified, fiber reinforced repair mortar, suitable for interior or exterior use, and containing corrosion inhibiting admixture. Material shall have the following properties neat:

1.	Compressive Strength minimum 2,000 psi (13.8 MPa) at 3 hours, minimum 3,000 psi (20.7 MPa) at 1 day and minimum 4,500 psi (31.0 MPa) at 7 days and minimum 6,000 psi (41.4 MPa) at 28 days per ASTM C 109, 2” (50 mm) cubes

2.	Flexural Strength minimum 600 psi (4.1 MPa) at 28 days per ASTM C 348

3.	Length Change maximum -0.02% at 28 days per ASTM C157

4.	NSF/ANSI 61 Standard Certified

5.	Basis of Design Product:

- Euclid Chemical Company (The); EUCOREPAIR V100  www.euclidchemical.com

B.	Manufacturer shall have ISO 9001 Quality Certification.

C.	To ensure compatibility bonding agent and curing compound when used shall be from same manufacturer as repair mortar.

2.___	CURING

{Euclid Chemical suggests curing this repair mortar with a high-solids curing compound. If desired choose a recommended product from the data sheet and insert a product description here. Guide spec language for these products can be found by accessing each product separately through the Euclid Chemical web site.

Be advised that liquid curing compounds are typically not compatible with future penetrating sealer, adhesives or coatings. If such treatments are intended the specifier should insert language for a dissipating resin curing compound such as KUREZ DR VOX or insert language for proper ACI 308 curing methods. Duration of such cure should be minimum 3 days.

When curing EUCOREPAIR V100 in potable water vessels, it is recommended to wet cure for 3 days, followed by 4 days of air cure prior to filling the vessel.}

PART 3.0	EXECUTION

3.___	SURFACE PREPARATION

A.		Concrete Removal: Remove all loose and unsound concrete per recommendations of ICRI Guideline 310.2R “Selecting and Specifying Concrete Surface Preparation for Sealers, Coatings, Polymer Overlays and Concrete Repair”

1.	Areas to be repaired shall have perimeter boundaries saw cut to minimum depth of ½ inch or less if such depth will cause saw to come in contact with embedded reinforcing steel.  Saw cuts shall be made perpendicular to the concrete surface and all concrete removal boundaries shall be straight and aligned parallel to opposite boundary edges resulting in repair areas that are rectangular in shape. The aspect ratio of the repair area shall be as square as possible, not exceeding 1.5:1. Odd shapes shall be avoided. If they cannot be avoided, re-entrant corners shall be mitered or reinforced to limit cracking at these locations.

a.	Extend repair boundaries to beyond corrosion on reinforcing bars.

b.	Do not allow saw to come into contact with reinforcing steel.

2.	All concrete shall be removed from within repair boundary to a uniform depth. Depth of removal shall be as required to accommodate manufacturer’s recommended minimum and maximum placement depth range for specified repair mortar and as required to remove all delaminating, cracking or unsound materials. Provide a sound surface with suitable profile for bond, as defined in repair mortar manufacturer’s written recommendations.

B.        Preparing Reinforcing Steel: Clean and prepare any exposed embedded reinforcing steel per recommendations of ICRI Guideline 310.1R. “Guideline for Surface Preparation for the Repair of Deteriorated Concrete Resulting from Reinforcing Steel Corrosion”

1.	Where ½ or more of diameter of reinforcement steel is exposed either by existing conditions or concrete removal, bond between the concrete and reinforcing steel is broken, or corrosion is present, the concrete shall be removed to provide a minimum ¾ inch clearance around entire perimeter of steel and along entire exposed length.

2. 	Remove concrete fragments, corrosion product, mill scale, and other contaminants from reinforcing bars in accordance with SSPC-SP 6 until a bare metal finish has been achieved on the reinforcing bars.

a.	Where section loss on a reinforcing bar is more than <<insert number>>percent, or <<insert number>>percent in two or more adjacent bars contact Engineer.

b.	Any damage to epoxy-coated reinforcement shall be repaired by coating with an approved epoxy-coating repair material.

C.	Remove bruised concrete substrate weakened by microcracking by abrasive blasting or high-pressure water blasting with or without abrasive.

D.	Concrete Preparation and Cleaning: Areas to receive concrete repair shall be structurally sound and free from deteriorated concrete, dust, dirt, debris, loosened concrete and aggregates, bruised concrete substrate weakened by microcracking, paint, oil, efflorescence, laitance, and other contaminants, and shall have a minimum Concrete Surface Profile CSP equal to that recommended by the repair mortar manufacturer per ICRI Guideline 310.2.

3.___	BONDING AGENT APPLICATION

{Note to Specifier: If a separate Euclid bonding agent is to be specified. Insert bonding agent execution language hear.}

3.___	REPAIR MORTAR APPLICATION:

A.	At areas where a bonding agent has not been specified, the saturated-surface dry (SSD) concrete shall be primed with a scrub coat of the specified repair mortar.

1.	Soak the repair area with potable water to achieve a saturated-surface dry (SSD) condition. Remove all puddled water from surface prior to application of scrub coat.

2.	The repair mortar must be applied before the scrub coat dries out.

B.	Repair Mortar Trowel Applied: Mix and place Repair Mortar per manufacturer’s recommendations within the open time of the product scrub coat or any bonding agents. Finish to level of surrounding concrete surface utilizing techniques recommended by manufacturer.

3.___	CURING

{Euclid Chemical suggests curing this repair mortar with a high-solids curing compound. If desired choose a recommended product from the data sheet and insert here. Guide spec language for these products can be found by accessing each product separately through this web site. Be advised that liquid curing compounds are typically not compatible with future penetrating sealer, adhesives or coatings. If such treatments are intended the specifier should insert language for a dissipating resin curing compound such as KUREZ DR VOX, a removable curing compound such as KUREZ RC, or insert language for proper moisture retaining curing methods meeting ACI 308. Duration of such cure should be minimum 3 days.

When curing EUCOREPAIR V100 in potable water vessels, it is recommended to wet cure for 3 days, followed by 4 days of air cure prior to filling the vessel.}

A.	Exposed repair mortar surfaces not receiving subsequent applications of penetrating sealers, coatings or adhesives, shall be cured utilizing a high-solids, water-based curing compound recommended by the repair mortar manufacturer.

1.	Under hot, windy or direct sunlight situations apply a second coat of curing compound.

B.	Liquid curing compound shall not be applied to surfaces that are to receive subsequent applications of penetrating sealers, coatings, or adhesives. Instead cure surfaces utilizing wet cure methods per ASTM C308.1 for minimum 3 days.

END GUIDE SPEC