VANDEX PLUG

Rapid Setting Crystalline Hydraulic Cement Repair Mortar For Repairing Active Water Leaks

{Note to Specifier: The paragraphs below are meant to be incorporated into Parts 2 and 3 of a standard CSI 3 Part Format specification, project’s General Structural Notes or directly onto the plans. They must be carefully reviewed by a qualified design professional and edited to meet the particular requirements of the project at hand, assure compliance with any governing building codes, and coordinate with other specification sections and drawings.}

PART 2.0:	PRODUCTS

2.__	CEMENTITIOUS REPAIR MORTAR

A.	Fast setting hydraulic cement repair mortar for repairing active water leaks. Provide prepackaged product with the following properties:

1.	Compressive Strength minimum per ASTM C 109

1 hour		1,000 psi

1 day		1,500 psi

28 days		3,000 psi

2.	Flexural Strength minimum per ASTM C 78

7 days		300 psi

28 days		350 psi

3.	Expansion/Shrinkage per ASTM C 157

Moist Room 100% RH	0.10%

Dry Room 50% RH	-0.25%

4.	Product:

a)	Euclid Chemical Company (The); Speed Plug, www.euclidchemical.com

B.	Manufacturer shall have ISO 9001 Quality Certification. To ensure compatibility, all associated products shall be from the same manufacturer.

PART 3.0:	EXECUTION

3.___	SURFACE PREPARATION

- Concrete surfaces must be structurally sound, free of loose or deteriorated concrete and free of dust, dirt, paint, efflorescence, oil and all other contaminants. Mechanically abrade the surface to achieve a surface profile equal to CSP >3 in accordance with ICRI Guideline 310.2. Properly clean profiled area.

- Mix product in accordance with manufacturer’s written instructions.

3.___	APPLICATION:

- Areas to be repaired shall be in a saturate surface-dry (SSD) condition using potable water immediately before application of VANDEX PLUG.

- Follow manufacturer’s written application instructions.