VANDEX CEMELAST

Elasticized Waterproof Coating

{Note to Specifier: The paragraphs below are meant to be incorporated into Parts 1, 2, and 3 of a standard CSI 3 Part Format specification, the General Structural Notes, or directly onto the plans. They must be carefully reviewed and edited by a qualified design professional to meet the requirements of the project and governing building codes. Coordinate with other specification sections and drawings.}

PART 1:	GENERAL

1._	PRE-APPLICATION MEETING

A.	Prior to the start of the waterproofing the General Contractor shall conduct a meeting to review the required methods and procedures to achieve the required placement. The General Contractor shall send a meeting agenda to all attendees 20 days prior to the scheduled date of the meeting.

B.	The contractor shall require responsible representatives of every party concerned with the waterproofing work to attend the meeting, including but not limited to the following: General Contractor’s Superintendent, waterproofing contractor, waterproofing manufacturer, and Owner’s Representative.

C.	Minutes of the meeting shall be recorded, typed, and distributed by the General Contractor to all concerned parties, including but not limited to the Owner’s Representative, the Architect, and all attendees within 5 days of the meeting.

PART 2:	PRODUCTS

2.__	Elasticized Waterproof Coating:

A.	Elasticized Waterproof Coating comprised of 2 components for positive side waterproofing.

1.	Euclid Chemical Company (The); Vandex Cemelast, www.euclidchemical.com

a)	Vandex BB 75

b)	Vandex Cemelast Liquid

2.__	Manufacturer shall have ISO 9001 Quality Certification.

PART 3:	EXECUTION

3.__	Elasticized Waterproof Coating:

A.	Honeycombs, cracks, cavities, voids, tie holes, and other defects shall be opened and routed to ¾” or to sound concrete.

B. 	The surface must be structurally sound, clean and free of dirt, oil and other contaminants including curing compounds, form release agents, old coatings, paint and efflorescence. New concrete and masonry must be cured a minimum of 7 days. All concrete laitance must also be removed. Provide an absorptive surface (CSP 1-3 in accordance with ICRI Guideline 310.2) on all substrates including precast and formed concrete.

C.	Concrete substrate shall be SSD.

D.	Mix, apply, finish, and cure Elasticized Waterproofing Coating per manufacturer’s written recommendations.